## Slide 1: Technology Roadmap for CMOS Manufacturing Industry
Dr. Qian Fan

## Slide 2
Resume

## Slide 3
Semiconductor Industry
Application
Hardware
Semiconductor Manufacture
Material
Material: Si, Ge, C, GaAs, InP, GaN, ZnO, ZnSe, ….
Manufacture: Analog, CMOS, MEMS, Photonics, CCD, LD/LED, ….

## Slide 4
Complementary metal–oxide–semiconductor (CMOS)
Typical circuit design uses symmetrical pairs of n-MOS and p-MOS
Low static power consumption
Low noise
High density of logic functions
Vdd
Vss
A
A
Q

## Slide 5
Complementary metal–oxide–semiconductor (CMOS)

## Slide 6
Fabrication Technologies - Photolography
Photoresist: Photo sensitive, organic material, liquid.
Coating: Spin coating, surface preparation, baking.
UV light: Short wavelength, 436nm, 405nm, 365nm, 248nm, 193nm, 157nm, …….
Mask: quartz with Cr masking layer, made by laser writer or e-beam writer.
Reduction ratio: 1:1, 5:1
Developing: N(CH3)4 OH, Tetramethylammonium Hydroxide (TMAH)
(a)
(b)
(c)
(d)

## Slide 7
Fabrication Technologies – Ion Implantation
Certain material ions are accelerated in an electrical field and impacted into a semiconductor substrate.
p-dopant: B, As.
n-dopant: P.
ion current vs ion energy
Damage recovery.

## Slide 8
Fabrication Technologies – Chemical Vapor Deposition
It is a chemical process to produce high-purity, high-performance thin film materials. Those materials include SiO2, Si3N4, poly Si, SiGe, GaAs, GaN, W, TiN, HfO2, ZrO2, …
PECVD: Use plasma to enhance the chemical reaction rate, coverage and stress. SiO2, SiNx.
LPCVD: Low pressure, high temperature process to produce high quality film. SiO2, poly Si.
Metal CVD: CVD process to deposit metal films by cracking metal compound. W, Cu.
MOCVD: CVD process using metalorganic precursors. GaN, GaAs, InP.
ALCVD: Deposits successive layers of different substances to produce crystalline films. HfO2, ZrO2.

## Slide 9
Fabrication Technologies – Chemical Vapor Deposition
PECVD
LPCVD
MOCVD

## Slide 10
Fabrication Technologies – Physical Vapor Deposition
It is a physical process to deposit thin film materials in ultra-high vacuum. Majority of such materials are metal: Ti, Ni, Au, Cr, Cu, Al, Pt, Ge, TiN, ITO, …
Evaporator : Metal source is heated to a vapor by electron bombardment in high vacuum, and condensed on the substrate.
Sputter: Source material is sputtered away by plasma discharge bombardment, and re-deposit on substrate.
E-beam evaporator
Sputter

## Slide 11
Fabrication Technologies – Plasma Dry Etching
Plasma dry etching refers to the removal of material by exposing the material to a bombardment of plasma ions. Removal mechanism involves both chemical reaction and physical bombardment.
Dry etching
Wet etching
Fluorine plasma: CHF3, CF4, C2F8, … to etch Si, SiO2, SiNx,
Chlorine plasma: Cl2, BCl3. To etch Al, Cu, Ti, Cr, TiN, GaN, GaAs, InP, …
Oxygen plasma: O2, to etch polymer type of material.
Ar, N2 plasma: purely physical bombardment to remove material.

## Slide 12
Fabrication Technologies – Chemical Mechanical Polishing
Chemical Mechanical Polishing is a process of smoothing surfaces with the combination of chemical and mechanical forces.
Material to polishing: SiO2, Si3N4, Si, W, Cu, Al, Ni…

## Slide 13
Moore’s Law
The number of components on IC doubles approximately every two years.

## Slide 14
Technical Difficulties
The technical difficulties when moving from sub-micron to deep sub-micron technology nodes:
Deep UV Lithography
Speed (mobility of electron/hole)
Gate leakage
Power consumption
CD: critical dimension; λ: wave length, NA: numerical aperture
Gate dielectric thickness ~1.7 nm for 35nm gate N-MOS transistor

## Slide 15
New techniques – Deep UV lithography
Stepper (scanner)
TEM top plan view on a single cell
Xilinx Kintex-7 FPGA
Manufactured by TSMC

## Slide 16
New techniques – Deep UV lithography
Immersion lithography
Resolution Enhancement Technology (RET)
Optical Proximity Correction (OPC)
II
I
III

## Slide 17
New techniques – Strain engineering
To increase mobility of electrons (holes) under the gate in MOS transistor, by adjusting the strain (energy band structures) ) in semiconductor. For Si industry, strained Si and SixGe1-x are often implemented to adjust the mobility.
Vd: drifting velocity
u: mobility
E: electrical field
Carrier mobility is related with band structure, doping, crystal defects, temperature etc.
Si grown on SiGe has lattice mismatch, which results in the changing of band structure in strained Si. Both carrier density and mobility can be increased.
mobility ~ speed of the device

## Slide 18
New techniques – Strain engineering
TEM cross section view on a single transistor of
Qualcomm Snapdragon S3 mobile processor
Manufactured by TSMC

## Slide 19
New techniques – High k dielectrics
SiO2 has been used as a gate dielectric material for CMOS since 1970’s. As transistors have decreased in size, the thickness of gate dielectric has steadily decreased to increase the drive current, raising device performance. As the thickness scales below 2 nm (45nm technology node), leakage currents increase drastically, leading to high power consumption and reduced device reliability.
Candidate: HfO2, ZrO2, HfSiO4, ZrSiO4
Deposition method: Atomic layer deposition
Considerations:
Film quality (electrical defects)
film morphology
thermal stability
Effect to carrier mobility
Deposition rate
Electron
Electron
Dielectric (barrier)

## Slide 20
New techniques – Fin FET
In FinFET, the conducting channel is wrapped by a thin silicon "fin", which forms the body of the device. The thickness of the fin (measured in the direction from source to drain) determines the effective channel length of the device.
Advantages:
Lower leakage currents caused by a fully depleted channel region
Reduced short-channel effects
More transistors/unit area due to 3D layout
Less variation effects from dopant fluctuation
Lower retention voltage in SRAMs

## Slide 21
New techniques – Fin FET
Intel patented nonplanar transistor architecture: Tri-gate transistor

## Slide 22
New techniques – Silicon on insulator (SOI)
Silicon on insulator (SOI) technology refers to the use of a layered silicon-insulator-silicon substrate in place of conventional silicon substrates in semiconductor manufacturing.

## Slide 23
New techniques – Silicon on insulator (SOI)
SOI + Strain engineering
The way to produce SOI wafer:
H2 implantation + wafer bonding + wafer polishing.
O2 implantation + thermal annealing.
SOI applications

## Slide 24
What’s the next technology to ensure Moore’s law ?
Next generation technology – 3D IC

## Slide 25
Next generation technology – 3D IC, die to wafer attaching
Bulk Si
CMOS layers
Carrier
Bulk Si
Memory device
Processor device
(a)
(b)
(c)
(d)
(e)
(f)
(g)
(h)
(i)
(j)
(k)
(l)

## Slide 26
Next generation technology – 3D IC, wafer to wafer attaching
SOI
CMOS layers
Bulk Si
(a)

## Slide 27
Technology development for 3D IC
Through Si via (TSV)
Next generation technology – 3D IC
Fluorine chemical based deep reactive-ion etching (DRIE), which is a highly anisotropic etch process used to create deep holes.
Bosch process, pulsed plasma dry etching process:
Step a: Sulfur hexafluoride (SF6) plasma is often used for silicon etching.
Step b: Octafluorocyclobutane (C4F8) to passivate the sidewall.

## Slide 28
Technology development for 3D IC
wafer thinning down
Next generation technology – 3D IC
Wafer backgrinding.
Wafer lapping.
TTV (total thickness variance) control
Carrier wafer bonding/debonding.

## Slide 29
Technology development for 3D IC
Deep via dielectric deposition
Via metal fill
Next generation technology – 3D IC

## Slide 30
Technology development for 3D IC
Aligned bonding
Next generation technology – 3D IC
a. Plasma activated fusion bonding.
b. Metal bonding
c. Adhesive bonding
d. Eutectic bonding
(b) Cu-Cu bonding
(d) Si-Au alloy eutectic bonding
(c) SU8 adhesive bonding
(a) SiO2-SiO2 fusion bonding

## Slide 31
Disadvantages of 3D IC
Yield Each extra manufacturing step adds a risk for defects. In order for 3D ICs to be commercially viable, defects could be repaired or tolerated, or defect density can be improved.
Heat Heat building up within the stack must be dissipated. This is an inevitable issue as electrical proximity correlates with thermal proximity. Specific thermal hotspots must be more carefully managed
Design complexity Taking full advantage of 3D integration requires sophisticated design techniques and new EAD tools
TSV-introduced overhead TSVs occupies the floorplan of IC layout
Testing To achieve high overall yield and reduce costs, separate testing of independent dies is essential
Lack of standards
Next generation technology – 3D IC

## Slide 32
Next generation technology – 3D IC
2.5D IC, Si interposer process flow, from Samsung.
2.5D IC vs 3D IC

## Slide 33
Semiconductor Industry
Application
Hardware
Semiconductor Manufacture
Material

## Slide 34
Semiconductor Industry

## Slide 35
Semiconductor Industry - Intel